# Spec Elite I Auto – Black TiNi

“Just good enough” and “too fast” are not words in our vocabulary. Producing top-of-the-line products for professionals is what we do. The Spec Elite series is one go-to blade when things get serious.

Like the Pentagon series, the Spec Elite series is designed as a backup and go-to tool for military and law enforcement personnel. Instead of a partially serrated spear point blade, the Spec Elite employs a clip point blade with a straight edge made in high quality AUS-8 steel. Extremely lightweight, the Spec Elite Auto features a hard anodized machined aluminum handle that provides sensational feel and balance. The Spec Elite Auto is an automatic knife intended for military and law enforcement. It can be carried conveniently with its reversible low-carry pocket clip.

## Key Selling Features:

Automatic knife designed for Military and LE Personnel

3.5-inch straight edge AUS-8 stainless steel blade

Hard Anodized Machined Aluminum Handle

Reversible low-carry pocket clip

Overall length: 7.8-inches, Weight: 2.8 ounces, Lifetime Warranty

FINISH			HARDCASED BLACK TINI

BLADE SHAPE		CLIP POINT

EDGE TYPE		STRAIGHT

BLADE STEEL TYPE		AUS-8

HANDLE MATERIAL		ANODIZED ALUMINUM 6061-T6

HARDNESS		RC. 57-58

PRODUCT WEIGHT		2.8 OZ

BLADE LENGTH		3.5”

CLOSED LENGTH		4.3”

OVERALL LENGTH		7.8”

MODEL NUMBER		SE-52

UPC			729857995740